## Slide 1: Spin-lattice relaxation of individual lanthanide ions via quantum tunneling
Fernando LUIS
Orlando
December 20th
2010
Quantum Coherent Properties of Spins-III Workshop

## Slide 2
Spin-lattice relaxation
T
Spin ensemble
Thermal bath
(phonons)
Spin-lattice interaction
h
P. Curie P. Ehrenfest
(1892) (1919)
P. Curie, Comptes Rendus Acad. Sci. (France) 115 805-808 (1892)
P. Ehrenfest, Leiden Commun. Suppl. 4b (1919).

## Slide 3
Phonon emission and absorption
Equilibrium
DEcb
DEba
Kronig, R. de L., Physica 6, 33 (1939).
Van Vleck, J. H., Phys. Rev. 57, 426 (1940).
R. Orbach, Proc. Roy. Soc. (London) A264, 456 (1961)
Orbach
Direct
1/t (s-1)
1/T (K-1)

## Slide 4
Phonon emission and absorption
Equilibrium
DEcb
DEba
Van Vleck (1940)
Kronig, R. de L., Physica 6, 33 (1939).
Van Vleck, J. H., Phys. Rev. 57, 426 (1940).
R. Orbach, Proc. Roy. Soc. (London) A264, 456 (1961)

## Slide 5
Mononuclear single-molecule magnets
LnW10
LnW30
Lanthanide (Er, Ho, Gd, Tm…)
Polyoxometalate moiety
Some outstanding characteristics…
Simple (just 1 magnetic atom)
Weak interactions
Magnetic solubility
Nuclear-spin free systems
Control over parameters
M. A. AlDamen et al, J. Am. Chem. Soc. 130, 8874 (2008)
17.9 Å

## Slide 6
Tailoring the magnetic anisotropy by chemistry: the case of Gd
GdW10
GdW30
Gd: [Xe]4f7
L = 0, S = 7/2
?
Model crystal-field probe

## Slide 7
GdW10
S = 7/2
g = 2
GdW30
S = 7/2
g = 2

## Slide 8
GdW10
S = 7/2
g = 2
GdW30
S = 7/2
g = 2
B20/kB = -0.059 K
B44/kB  4  10-4 K
B20/kB = +0.019 K
B22/kB  +0.019 K

## Slide 9
Easy axis
Jz
D/kB = 10-6 K
D/kB = 10-4 K
Jy
Easy plane
4 K
0.5 K

## Slide 10
M. J. Martíınez-Pérez, J. Sesé, F. Luis, D. Drung, T. Schurig, Rev. Sci. Instrum. 81, 016108 (2010).
GdW10
GdW30

## Slide 11
Long-range magnetic order: TN  20 mK
xdip/kB  0.02 K
Above TN, cT follows Curie-Weiss law
t is a SLR time

## Slide 12
T > 0.1 K:
Thermally activated
Agrees with Orbach process
109
T < 0.1 K:
Independent of T
8-9 orders of magnitude faster than direct processes

## Slide 13
J = 15/2
g = 6/5
~ 45 K
B20/kB = -1.35 K; B40/kB = -1.07  10-2 K; B60/kB = 1.67  10-4 K
B44/kB  1.8  10-2 K
Strong uniaxial anisotropy
Spin-lattice relaxation and quantum tunneling the case of Er
ErW10
SMM behaviour below 5 K
AF order at TN = 80 mK
M. Aldamen et al., Inorg. Chem. 48, 3467 (2009)
F. Luis et al., Phys Rev. B 82, 060403(R) (2010)

## Slide 14
109
F. Luis et al., Phys Rev. B 82, 060403(R) (2010)

## Slide 15
What about tunneling then?
D/kB  10-4 K
sdip  0.08 K
Tunneling
Direct process
N. V. Prokof’ev and P. C. E. Stamp, Phys. Rev. Lett. 80,
5794 (1998).

## Slide 16
Effect of a magnetic field
xdip = -xZeeman
xZeeman

## Slide 17
Effect of a magnetic field
xdip = -xZeeman
xZeeman
Direct process

## Slide 18
Spin concentration ErxY1-xW10
Er
Y

## Slide 19
Er3+: Kramers ion (J = 15/2)
D = 0 at zero field
Hdipx are required to break
Kramers degeneracy
Increasing
sdipx
D  x
sdip x
Gtun  x
Gtun  x2

## Slide 20
Hyperfine interactions 167ErW10
I = 0
164Er,166Er
168Er,170Er
I = 7/2
A/kB = -610-3 K
167Er
D  0

## Slide 21
Hyperfine interactions 167ErW10
xdip = -xhyperfine

## Slide 22
Strong hyperfine interactions HoW10
(1)
(1)
(1)
(2)
(2)
(2)

## Slide 23
T > TN
T < TN
xdip >> D
Relaxation vs long-range order: ErW10
TN = 81 mK
The onset of long-range order blocks QT and relaxation

## Slide 24
Aging: monitoring the growth of spin-spin correlations
time
t1
t2
t3

## Slide 25
T
Spin ensemble
Thermal bath
(phonons)
t-1
QT spin reversal vs spin lattice relaxation
QT flips the spins but conserves energy of the spin ensemble
How is energy exchanged with the thermal bath then?

## Slide 26
Zeeman
bath
Dipolar
bath
Phonon
bath
t-1dir
Gtun
t-1SR
Collective emission of phonons: phonon superradiance
H. N. V. Temperley, Proc. Camb. Phil. Soc. 35, 256 (1939).
E. M. Chudnovsky and D. A. Garanin, Phys. Rev. Lett.
93, 257205 (2004).

## Slide 27
Conclusions
Mononuclear SMM: tailoring the energy level structure with chemistry  magnetic coolers, qubits, …
Nearly quantitative agreement between measured tunneling rates and theory
Quantum spin tunneling provides a very efficient mechanism of spin-lattice relaxation
Puzzle: energy flow between spins and the lattice
?

## Slide 28
Javier Sesé
Mª José Martínez
David Zueco
Agustín Camon
Marco Evangelisti
Oscar Montero
Enrique Burzurí
Thomas Schurig
Dietmar Drung
Salvador Cardona-Serra
Carlos Martí-Gastaldo
Juan Modesto Clemente
Eugenio Coronado
Joris van Slageren
Christoph Schlegel